## Slide 1: Overview of Materials Developments In the Target Fabrication Group at LLNL
23rd Target Fabrication Specialist Meeting
Annapolis, Maryland
April 23rd, 2019
Suhas Bhandarkar
for LLNL Target Fabrication S&T Group

## Slide 2: LLNL Target Fab S&T retains a dedicated pool of experts. It leverages capabilities in other directorates as well as maintains close collaborations with external partner institutions
Foams
Metrology & Spectroscopy
Advanced Materials & Processes
Precision Machining
Additive Manufacturing
Vapor Processing Lab
TEM/FIB
Beamline measurements
Tomography
Soft Matter/ Nanomaterials
Coatings
Target Fab

## Slide 3: Our mission is to pursue both long-term and short-term R&D based on Physics priorities
Better ablator materials
Mitigate capsule support perturbations
Mitigate the fill tube perturbations
Improve drive symmetry thru hohlraum modifications
Develop new materials and characterization capabilities
Inertial confinement fusion
Though these overall categories require long term attention and don’t change frequently, we work with HED/ICF Physics to fine-tune the priorities of new ideas and directions within each
Precision machining & coining
Glueless bonding
Pu processing, machining & bonding
Foam development, shaping and machining
X-ray sources development
New materials and processes
High energy density physics

## Slide 4: We have embarked on a number of key initiatives to develop necessary materials and technologies for upcoming and future targets
Here, I will complement the technical highlights that Abbas presented previously with a S&T overview
Nano crystalline diamond (NCD)
Smoother Be shells
Tetracage with C-nanotube yarns
‘Fishing pole’
Superconducting coatings
2um FT
Use of foams in hohlraums
New hohlraum designs (Iraum, Rugby, Frustraum)
High Z Metal shells by eplating
Fine grained metal alloy shells (HiPIMS)
Eplating unique metals using ionic liquids
AM templated & Nano-porous Au foams
Nanowire synthesis & foams
Cryogenic hydrogen R&D
Particle detection & location from X-ray images
Ion-beam analysis
X-ray reflectometry & phase cont. comp. tomography
Nano-joining materials using iCVD
Glueless bonds for metals
Pu machining
Sub-micron Pu bonds

## Slide 5: HDC capsules with nanocrystalline (NCD) structure were produced recently and shot on NIF for the first time
Despite being in production, HDC shells still require substantial R&D to reach maturity
Work by J. Biener & M. Stadermann in collaboration with Diamond Materials & GA
New void-free NCD shells: reproducible growth & dopant levels
Undoped NCD
W-doped NCD
KC463
interface
SAD
150 nm aperture
Previous shells were micro-crystalline with columnar morphology
10um
As grown surface
Growth direction
KC247
Lateral grain size 2-5 µm
EBSD grain orientation map
Further refinement of grain size
Flats
Shells
Velocity from planar HDC with different grain sizes

## Slide 6: We are developing new methods for making hollow spheres through deposition of thick, dense, leak-tight metal coatings with low stress
HiPIMS
DCMS
Cr shell made with HiPIMS, an emerging technique for controlled microstructure
Developing reliable fabrication of target-quality shells generally takes many years of sustained effort
Interesting possibilities of making new pure & alloyed metal shells through both aqueous & ionic liquid electroplating
E’plated metal & metal alloy shells
Ionic liquids expand possibilities
Engwall, Tues 1:50pm
Peters, Thurs 9:10pm
Horwood, Thurs 9:30pm
Also Kucheyev, Wed 2:30pm on superconducting coatings
Electrochemistry
Sputtering

## Slide 7: Beyond the demonstration of transparent capsules, iCVD is being used for exploring nano-bonding
Thin Solid Films 635, 2017, 37-41
5 μm
Pb
V
Ultrathin solid adhesive
Foil or foam
SiC
SiC
384 nm
Epoxy type polymers with low Tg deposited via iCVD for thin bondlines
Transparent plastic shell 1 mm dia made using iCVD
Work by X. Lepro-Chavez, S. Baxamusa et al

## Slide 8: There are wide-ranging applications of ultra-low density foams in targets and we have a broad portfolio of new templating (& nanowire freeze-extract) methods to make a variety of shapes
Advanced hohlraum design
hohlraum
capsule
foams of different density
Specialized foam-lined hohlraums
Foam shells for interfacing with capsules
27mg/cc tantala
Low density foams using 2PP writing yield unique microstructures and designer shapes
Foams fabricated using nano-porous Au as a template
Work by M. Biener
Oakdale, Wed 1:30pm
Also Fears, Thurs 3:10pm on nanowire foams

## Slide 9: Cryogenic ice team has been instrumental in enabling and sustaining a layered shot per week
Layered shot rate has been near double over the past 2 years despite more non-standard targets
RRI (refraction enhanced imaging)
Compton Radiography
HT layers in targets for new imaging approaches
CBI (crystal backlit imaging)
‘Fang’ target with a minimal side-view (no starburst arc)
Kroll, Thurs 2:30pm
Fielding a target with 2um required careful gas handling procedures (pump-purge, etc)
2um FT

## Slide 10: S&T team has been expanding our capabilities for making high quality layers at a range of ice thicknesses with good modal control
DT layer thickness has been recently pushed to its lower limit (<20um)
<20um
Filltube
Thinner
Thicker
Measurement of cryogenic thermal impedance of the Al TMP-Si bond is key for better low modes
Test sample for thermal impedance measurement for improving the bond performance
Work by J. Sater et al
Wray, poster
Cryogenic thermal conductivity
Thin DT ice layers

## Slide 11: We continue to work on the high degree of cleanliness required for targets, both on characterization and mitigation of flaws that can potentially affect capsule implosion
# | Location | X | Y | Area (um^2)
1 | Bottom LEH | 466.1 | 980.2 | 89.8
2 | Capsule | 250 | 929.8 | 31.4
3 | Capsule | 489.1 | 522.1 | 37.4
4 | Capsule | 746.1 | 993.1 | 41.9
5 | Capsule | 795 | 580.7 | 18.0
6 | Capsule | 274.4 | 786.4 | 19.5
We have developed an automated routine to detect and identify the spatial location of debris seen in X-ray images
We have embarked upon a systematic study of offending particles of target components
Walters, Wed 11:00 am
Braun, Fri 9:30am

## Slide 12: When needed, we leverage LLNL site-wide capabilities as well as advocate for their continued upgrade & expansion
µm-scale holes in TATB
Helios G4 P-FIB CXe
Multiple ion source
4-8x faster milling
Low damage
High resolution
10 nm FIB
1 nm SEM
New Plasma-FIB will greatly increase capability & throughput for microsculpting of capsules & foams
Ion beam analysis is critical for specific characterization
Shin, Thurs 11:40am

## Slide 13: Targets S&T project portfolio seeks to have relevant impact on HED/ICF program while seeking to explore underlying science
Significant contributions to drive new target types for important shots
  Smaller (2um) filltubes
  Capsule microstructure improvement
  Tentless capsule suspension techniques
  New hohlraum designs
  Design-specific fuel-ice, both composition and thickness
  New HED physics packages
Long-term efforts on metal shells, unique foams, growing options for ablator & hohlraum materials lay the groundwork for continued progress of the missions we support
(Kong, Thurs 9:50am ; Crippen, Thurs 1:30pm)
(Lepro Wed 2:10pm, Schiaffino Wed 2:50pm, Aracne-Ruddle, poster)