## Slide 1
W. Sweet, R. Jimenez, R.I. Mohammed, F.H. Elsner, K.J. Boehm, J.C. Williams, A. Garcia, R.R. Paguio, M. Ratledge, H. Huang, N.M. Ravelo, N.G. Rice, E. Mathison, H. Xu, P. Fitzsimmons, and M.P. Farrell
Improvements in CH Ablators Fabricated by Microencapsulation
General Atomics, P.O. Box 85608, San Diego, California 92186-5608
23rd Target Fabrication Meeting
Annapolis, Maryland
April 23-26, 2019
Work supported by General Atomics IR&D

## Slide 2: GA uses microencapsulation to fabricate many types of shells and beads
Microencapsulation overview
PAMS mandrels
Polystyrene capsules
Wetted foam fabrication

## Slide 3: Microencapsulation is a high volume technique for fabrication of polymeric shells
Shells cured & agitated in heated bath
Droplet
generation
Drying in a vacuum oven
Polymer Solution (O1)
Inner Water (W1)
Outer Water (W2)
Osmotic inner water removal
Steps
Droplet generation
Curing
Inner water removal & drying
Characterization
Hundreds to thousands of shells can be fabricated in a single batch

## Slide 4: Microencapsulation in the Droplet Generator

## Slide 5
Poly(α-methylstyrene) Shell Fabrication Status

## Slide 6: Last year, efforts have focused on ensuring the quality of the PAMS feed material
Unusually poor PAMS pyrolysis residue linked to one PAMS lot in 2017
Ensuring long term supply of residue-free PAMS is essential
Additional lots of PAMS from the existing supplier have been pre-qualified as residue-free—multi-year inventory of qualified material
Shells were fabricated from material from alternate vendors
Worked with the existing supplier to improve the quality of the material
Synthesis of small lots of PAMS at GA to ensure supply of high quality, residue-free PAMS
Examples of 2017 Pyro Residue

## Slide 7: Optical yield for GA-synthesized PAMS is already comparable to vendor-supplied material
GA-PAMS has typical optical passing rate
Lower pass rate for PAMS from an alternate supplier
2017
2018

## Slide 8: GA-fabricated PAMS material matches optical quality of supplier-provided PAMS
PAMS180226-A, Typical Vendor-Supplied PAMS
PAMS180226-E, GA-Fabricated PAMS
200 μm
200 μm

## Slide 9: “Star crack” reduction is another objective—will improve PAMS optical yield & quality of NIF GDP capsules
“Star/spider cracks” & depressions often form as a bubble nucleates during the removal of the inner water
PSDI data for GDP often has a single depression with dimensions characteristic of star cracks
Production PAMS shells rejected for star cracks:
  10-40% of PAMS shells with standard AZ100 culling
  ~30-60% of PAMS shells on new robotic culling station
~150 µm diameter 100 nm deep
NIF PSDI:
Fiducials added to star crack before coating
AZ100 image (No visible star cracks)
Robotic culling image (Visible star crack)

## Slide 10: Star cracks were assessed manually and with automated defect statistics from the AZ100
0
1
2
3
4
5

## Slide 11: Promising conditions for star crack reduction were identified
Replication & evaluation of AFM data is required before implementing as a production step
*A batch prone to cracking was used to make it easier to see trends. The batch was split and placed either in standard or R&D conditions.
Influence of Nucleation Conditions on Star Cracks

## Slide 12
Polystyrene Shell Fabrication Status

## Slide 13: Recent microencapsulation R&D efforts have focused on reducing vacuoles in PS shells
Polystyrene is of interest to LLE for the 100GBar Initiative as an inherently dome-free alternative to GDP
Process development has resulted in shells equivalent to or better than GDP for the following:
  Wall uniformity
  AFM
  Optical defects
Polystyrene Shell

## Slide 14: AFM is used to assess shell quality
Low Modes 2-6
Low Modes
Sphericity
Mid Modes 7-25
Mid Modes
Wrinkling
Isolated Defects
High Modes 26-150
High Modes
Small features
Roughness
Scratches
Power Spectrum
Raw Traces (Defect Examples)
High modes
Low modes
Mid modes

## Slide 15: PS shells have better low modes than typical GDP
GDP
GDP
Typical PS
Best PS
NIF Spec
NIF Spec
Typical PS vs. GDP
Best PS vs. GDP

## Slide 16: Low modes are consistently low for batches fabricated over a range of conditions
Comparison of AFM for Delivered GDP and Representative PS batches
GDP
Polystyrene Batches
Low Modes

## Slide 17: Dark field microscopy can be used to characterize submicron defects
0.49 µm Calibration Standard
GDP Shell
GDP Defects
H. Huang, J. Walker, K. Sequoia
In dark field microscopy of submicron defects, light intensity is a surrogate for size

## Slide 18: Quantitative dark field analysis is now being used for process feedback
PS shell (PS180213-B)
GDP (SCD52-V)
Outer surface
Inner surface
Outer surface
Artifact
Inner surface
Inner wall defect
With the improved dark field method, we can now determine that most defects cluster near the surface of the walls for both SCD and PS.
Defect position within wall
Map color indicates defect depth in wall
Depth (µm)
Defect Diameter (µm)
Depth (µm)
Defect Diameter (µm)
Defect Diameter (µm)
Position
Defect Diameter (µm)
Position
Wall

## Slide 19: Dark field defect counts of candidate batches are much lower than typical GDP
*Bars represent the batch average of the dark field defect count using one image per shell (~0.5% of surface area)
Record Low Defect Count
SCD (GDP)
PS

## Slide 20: Maximum dark field defect size in candidate batches has also been reduced
Median defect size
Max defect size
*Bars represent the batch average of the maximum defect size for one image per shell (~0.5% of surface area)
Old PS
New PS
SCD (GDP)

## Slide 21: Dark field analysis suggests some PS shells are close to meeting the current LLE defect specification
See also M. Bonino’s Talk
Unacceptable for current cryo spec
Unacceptable for 100GBar spec
Acceptable for 100GBar spec
Measured defects*
-C
-C

## Slide 22: Wall uniformity comparable to that of GDP was maintained for recent process conditions
GDP
PS
0.25 µm specification
Notes: Include more data here

## Slide 23
Foam Shells
From http://www.aerogel.org/?p=71

## Slide 24: GA Fabricated RF-lined GDP shells in support of LANL wetted foam project
The “inside-out” fabrication route for foam-lined shells has many challenges:
  Low modes: GDP coating is conformal—low RF shell out-of-round is essential
  Non-concentricity: RF shells are thicker and typically less uniform than PAMS
  Domes: RF has more surface roughness than PAMS. Anhydrous polishing process developed
LANL RF-lined GDP design
1 mm
RF shell
5 Day Polish
GDP
RF
Ref: B. Haines, Phys. Plasmas 26, 012707 (2019)

## Slide 25: Conclusions
Microencapsulation is a versatile technique used to mass-produce capsules from many materials
Current PAMS effort is focused on securing residue-free PAMS & on star crack reduction
Best ever PS shells were fabricated last year as a result of process improvements
Some strategies from PS shell development might be applicable to PAMS