## Slide 1: Diamond turning of High Tool Wear Materials for Equation of State Targets
Target Fabrication Conference 2019
Carlos Castro, L. Ahrendes, T. Matz, N. Le, D. Fratanduono, R. Seugling, A. Nikroo
April 2019

## Slide 2: Presentation Outline
Equation of State (EOS) Targets
Machining of EOS components
Why Diamond Tools for Machining
List of Diamond Turnable Materials
High tool wear materials Diamond Turned at LLNL
Other materials
Summary

## Slide 3: Equation of State (EOS) Targets
The gold hohlraum is driven top and bottom using the NIF laser to create an x-ray drive on the sample shown on the right. Part #1 is ablated causing a pressure wave through the stepped sample, part #2. The velocity of the stepped profile is measured using a velocity interferometric diagnostic (VISAR1). Variation in thickness and form correlate to a velocity error.
The figure shows a schematic of a planar target assembly where the sample is a combination of two thin foils machined independently and assembled using an adhesive.
Target Specifications:
The specification for the acceptable thickness variation for Equation of State (EOS) targets is defined using the Half Width Half Maximum (HWHM) of a Gaussian Distribution fitted to the histogram of the thickness data from a Region of Interest (ROI) on each component and the final assembled the physics package.
For the EOS targets the HWHM specification is 50nm.
The ROI for defining the HWHM is shown by the red dashed rectangle
HWHM
The blue arrow shows how the HWHM is defined

## Slide 4: Machining process of a stepped EOS sample
EOS samples are turned (machined ) off-axis
Samples are mounted on a Ø100 mm Disk using a soluble adhesive (multiple parts)
The work holding disk is held by vacuum on the lathe spindle
Samples are machined on both sides and have in-process WLI checks
Parts are then Machined to the specified thickness and profile

## Slide 5: EOS Target assembly specifications
Parts must be within 50nm of profile and parallelism
Assembly must be within 50nm parallelism
Parts must be measured independently using the Double-sided white light interferometry (DSWLI) before assembly
For the EOS targets the physics team asked Target Fabrication if we could reduce the HWHM from 100nm to 50nm. This would reduce the uncertainty of the data they get for each target shot on NIF by a factor of 2. Reducing the uncertainty by a factor of 2 reduces the number of targets that need to be shot by a factor of 4, saving 3 shots for each data point.
EOS assembly station with force sensor

## Slide 6: Why do we use Single Crystal Diamond Tools for Target Fab
We use diamond tools to manufacture high precision components – Typical machine tool (Diamond Turning Lathe) has submicron positioning and contouring <.010um precision
We use diamond tools to machine small features on Target components – Zero tool tip radius used in gratings
We use diamond tools to achieve specified surface roughness – < 5nm Ra typical
10X
20X
100X
Carbide 100umR
CBN 250umR
Diamond single crystal 25umR
Diamond Endmills

## Slide 7: List of diamond turnable materials: “Chemical Aspects of tool wear in single point diamond turning”
Mr. C.J. Evans
Precision Engineering Division
National Inst. Of Standards and Technology
Metrology A 107 Blg 220, Quince Blvd
Gaithersburg MD 20899, USA
January 1996
Data for elements with know diamond turning properties |  |  |  |  | Diamond Turnable? | 
Element |  | Melting Point c° | Microhardness kg/mm² | No. of unpaired d-shell electrons | Yes | No
In | Indium | 157 | 10 | 0 | Yes | 
Sn | Tin | 232 | 9 | 0 | Yes | 
Pb | Lead | 373 | 5 | 0 | Yes | 
Zn | Zinc | 420 | 51 | 0 | Yes | 
Pu | Plutonium | 640 |  | 0 | Yes | 
Mg | Magnesium | 649 | 48 | 0 | Yes | 
Al | Aluminum | 660 | 25 | 0 | Yes | 
Ge | Germanium | 937 | 721 | 0 | Yes | 
Ag | Silver | 962 | 96 | 0 | Yes | 
Au | Gold | 1064 | 96 | 0 | Yes | 
Cu | Copper | 1083 | 76 | 0 | Yes | 
U | Uranium | 1132 |  | 1 |  | No
Mn | Manganese | 1244 | 384 | 5 |  | No
Be | Beryllium | 1277 |  | 0 | Yes | 
Si | Silicon | 1410 | 1211 | 0 | Yes | 
Ni | Nickel | 1453 | 189 | 2 |  | No
Co | Cobalt | 1495 | 247 | 3 |  | No
Fe | Iron | 1535 |  | 4 |  | No
Ti | Titanium | 1660 | 142 | 2 |  | No
Cr | Chromium | 1857 | 250 | 5 |  | No
V | Vanadium | 1890 | 248 | 3 |  | No
Rh | Rhodium | 1966 |  | 2 |  | No
Ru | Ruthenium | 2310 |  | 3 |  | No
Nb | Niobium | 2468 | 128 | 4 |  | No
Mg | Molybdenum | 2617 | 192 | 5 |  | No
Ta | Tantalum | 2996 |  | 3 |  | No
Re | Rhenium | 3180 | 319 | 6 |  | No
W | Tungston | 3410 | 348 | 4 |  | No
Data for selected elements with unkown diamond turning properties |  |  |  |  |  | 
Sb | Antimony | 631 |  | 0 |  | 
Y | Yttrium | 1522 |  | 1 |  | 
Pt | Platinum | 1772 |  | 1 |  | 
Ir | Iridium | 2443 |  | 3 |  | 
Several mechanisms can contribute to tool wear and they can work simultaneously
Adhesion and formation of a built-up edge
Abrasion, microchipping, fracture
Tribochemical wear
Chemical tool wear is when carbon atoms are pulled from the tightly bonded diamond lattice. Once an atom leaves the diamond, it may diffuse into the work piece, graphitize, or react with the oxygen or the work piece to form a carbide.

## Slide 8: Machining of Iridium for EOS targets
Stock Surface
Diamond Turned surface
Cutting parameters
.025mm tool radius 80º included angle
1.0mm/min tool federate
.002mm depth of cut (DOC)
1000 rpm
Cut area 21mm² (20um total depth)
Cutting Fluid-Odorless Mineral Spirits
80°
Ø100mm Disk
Surface roughness 25nm Ra in turned area
Initial test cuts on Ir 99.7 % purity 25mm x 25mm foil from American Elements – (Dayne Fratanduono)
Legacy tools from LODTM 1970’s

## Slide 9: Process improvements reduced the number of tools per target
First Sample
Very high tool wear was observed during the machining of the stepped samples
14 natural diamond tools were used to machine the first stepped sample
5x Photo of finished sample 1mm reticle scale
10x Photo of finished sample 1mm reticle scale
.047um Ra
9.0um Step
.077um Ra
0.0um Step
.017um Ra
.019um Ra
Polycrystalline Diamond (PCD) tools were introduced to rough material
PCD tools were used to rough cut most of the material leaving only 4 um of material for the Diamond tool to finish cut the profile.
PCD tools exhibited much higher wear resistance than single crystal diamond tools.

## Slide 10
IrEOS Stepped sample and Region of Interest Results
IrEOS specimen;
< 50nm parallelism overall
< 15nm parallelism in ROI
2 PCD tools
2 Natural Diamond tools

## Slide 11
PtEOS specimen;
< 12nm parallelism overall
< 7nm parallelism in ROI
Platinum Stepped sample and Region of Interest Results

## Slide 12: Machining of Tantalum (manhole cover) for EOS targets
19.5 nm HWHF parallelism base on DSWLI
Process development
Initial tests 0° rake tools
Cutting fluid- EcoCut
Limited to 100nm depth of cut
Note: Legacy Ta tools +25° rake angle
We then partnered with tool vender to manufacture SPDT replaceable insert tools at +25° rake angle
Results
< 15nm Ra
300nm depth of cut
20nm HWHM in ROI
1972 Legacy carbide tool designed by LLNL for turning Ta
25º

## Slide 13: Machining of an Iron (99.99%) disk for diffraction targets TARDIS
Lapping and polishing has resulted in very low yields.
DT was a last resort but offered a quick turnaround
16nm Ra Surface roughness measured on the white light interferometer (WLI)
100% yield (4 Disks)

## Slide 14: Machining of MgO for EOS targets
Tool Specification | Tool Radius | Tool Rake Angle | Depth of Cut (DOC) | Feed Rate (FR) | Total infeed | Surface Finish
Test Cut 1 | .025mm | 0° | .002mm | 5mm/min | .026mm | Part Shattered
Test Cut 2 | .150mm | 0° | .0005mm | 3mm/min | .010mm | .752um Ra
Test Cut 3 | .250mm | -30° | .0005mm | 3mm/min | .004mm | .242um Ra
Schafer Corp
3 Day Cut Study June 2016: 3 Test Cuts

## Slide 15
Tool Pass | Tool Radius | Tool Rake Angle | Depth of Cut (DOC) | Feed Rate (FR) | Laser Power | Surface Finish
1 | .250mm | -35° | .008mm | 4.25 mm/min | 25% | 128nm Sa
2 | .250mm | -35° | .006mm | 2.55 mm/min | 25% | 99nm Sa
3 | .250mm | -35° | .006mm | 2.55 mm/min | 35% | 79nm Sa
Customer: Schafer Corp
Test Date: 19-21st July, 2016
Test Location: Micro-LAM
Note:
1. Surface roughness readings were obtained using a Taylor Hobson CCI 6000
2. 4 readings were taken to cover multiple areas across the machined sample
3. Avg. Sa represents the average of the 4 roughness measurements (Sa 1…Sa 4)
4. The fact that Pass 3 yielded better surface finish then Pass 2 indicates that the tool was preserved and the additional laser power enhanced the ductility of MgO.
5. Sample machined uniformly across entire area
Micro-LAM’s Summary
Micro-LAM (Laser Assisted Machining) MgO Test Cuts- July 2016
Note:
Test cuts were duplicated without LAM. We were able to get similar surface finishes without LAM
Micro-LAM claims that their tool was preserved and the laser power enhanced the ductility of MgO

## Slide 16: Machining of MgSiO3 for EOS target
Photograph of as received sample (5x)
Sample has voids and possible inclusions
Photo of new PCD tool
PCD Test cut 10um material removed
Wear on PCD tool-not catastrophic
The finish cuts followed the PCD tool
The first finish cut was across the entire sample. A 70nm Ra surface roughness was recorded using the white light interferometer (WLI). 4 microns of roughed material was removed
The second finish cut was only on half of the sample. An additional 4um of material was removed from one half of the sample, resulting in 40nm Ra surface roughness.
Photo of used diamond tool
Significant wear on diamond
Surface roughness
40nm Ra measured on WLI
Surface roughness
70nm Ra measured on WLI
Single crystal diamond Tests

## Slide 17: Summary
We have successfully diamond turned previously thought of as “Not diamond turnable” material
We are developing machining processes for high tool wear compounds
The technology offers experimenters new materials for target components (Hohlraum, liners, back-lighters)