## Slide 1: Toward quantum levitation of thermonuclear fusion fuel capsules
Sergei Kucheyev
April 24, 2019
TFM 2019
Annapolis, MD

## Slide 2: The team
LLNL
Bimo Bayu Aji
Alex Baker
Elis Stavrou
Anna Hiszpanski
Alyssa Maich
Scott McCall
David Steich
Sergei Kucheyev
LLNL summer students
Robert Jacob
Jacob Beckham
Dante O’hara
GA
John Bae
Jason Rodriguez

## Slide 3: Outline
Why levitate?
Levitation scheme
MgB2 film growth
  Mg vapor annealing
  Solid state diffusion in multilayers
Levitation force measurements
Flux pinning by radiation damage

## Slide 4: Tents can cause significant perturbation to the implosion
Radiograph
Simulated DT fuel at stagnation
Tent
Tent
Tent
capsule
Phys. Plasmas 23, 056302 (2016); ibid 25, 072705 (2018)
The ideal capsule support is via levitation

## Slide 5: The ideal capsule support is via levitation
Capsule is coated with thin (~100 nm) superconducting layer, with magnetic coils outside the hohlraum
The 1st step is the development of superconducting coatings

## Slide 6: Levitation is not a new concept
R. Kleiner and W. Buckel, Superconductivity (Wiley, 2016)

## Slide 7: Levitation has been considered for capsule support for decades but remained elusive

## Slide 8: Simulations predict levitation in a low-field magnetic trap
Lower magnetic pressure
Higher magnetic pressure
Upward Lorentz Force
Combined (i) electromagnetic, (ii) mechanical, and (iii) thermal simulations of Lorentz forces, magnetic pressures, current densities, and thermal loading.
Film thickness: 40-400 nm
B = 100-300 G
J = 10-1000 A/cm2
Lorentz force = 50-150 µN
Levitation height = 5-6 mm
Supercond. Sci. Technol. 31 (2018) 055006

## Slide 9: MgB2 is a promising material for superconducting levitation of ICF fuel capsules
Excellent superconducting properties
Low Z
“Simple” binary compound
Synthesis compatible with current ablator platforms
Material | Tc (K) | Jc (A/cm2) | Hc2 (T)
YBCO | 95 | <8e6 | >100
MgB2 | 39 | <1e9 | >50
Nb3Ge | 23 | <1e5 | <40
MgB2 lattice

## Slide 10: We have studied two film growth methods scalable to non-planar substrates in a non-epitaxial regime
Mg vapor annealing of B films @ >650 oC
Solid-state diffusion of B/Mg multilayers @<650 oC
Challenges:
High reactivity of both B and Mg
High vapor pressure and low sticking coefficient of Mg
Multi-phase stability of MgBx
Complexity of B chemistry
C
35 nm B
25 nm Mg
35 nm B
1
2
3
Most previous research on MgB2 films involved epitaxial growth (on SiC and Al2O3), not applicable to the coating of ICF capsules
Precursor B and Mg films were sputter deposited on carbon

## Slide 11
Boron films thinner than ~50 nm rapidly age
137 days @ RT in vacuum
Post-deposition anneal at 1000 oC stabilizes B films

## Slide 12: With vapor annealing, best results are for short anneals at 850 oC with RTA-like profiles
Supercond. Sci. Technol. 31 (2018) 055006; Appl. Surf. Sci. 448 (2018) 498.
Typical T(t) profile for YBCO
Supercond. Sci. Technol. 30 (2017) 095001
We studied simplest T(t) profile
Results non-trivially depend on annealing conditions

## Slide 13: Oxygen impurity is inimical to superconductivity of MgB2
Films with [O] >13 at.% are not superconducting
Tc scales linearly with [O] with a slope of ~3K/at.%
Films thinner than 55 nm do not follow this trend

## Slide 14: Vapor annealed MgB2 films with thicknesses <55 nm are smooth
540 C/min, 12 min@850 oC
160 nm MgB2
~40 nm RMS
Limitations of Mg vapor annealing:
High-temperature process (850 oC).
Limited to ~55 nm films; thicker films exhibit multiple nucleation, with ~10 nm wide crystallites and stress-related effects.
Role of surfactant-mediated epitaxy (Fe, Ni, and Cu)?
55 nm MgB2
~1 nm RMS

## Slide 15: MgB2 films can be made via low-T solid state-diffusion approach
C
35 nm B
25 nm Mg
35 nm B
1
2
3
The SSD approach requires much lower thermal budgets than Mg vapor annealing

## Slide 16: Nucleation and grain growth are rate limiting steps in MgB2 formation
Inter-diffusion kinetics suggests that nucleation and grain growth (rather than diffusion) are rate limiting steps.
The same activation energy in the entire temperature range studied (400-650 oC).
J. Appl. Phys. 125 (2019) 075306.

## Slide 17: We have developed a new method of levitation force measurements
B-field gradient generates levitation force in superconductor
Commercial superconducting magnet/cryostat provides fine control of temperature and magnetic field
Load cell at RT above the probe
Sample hangs on string above coils in B gradient

## Slide 18: Superconductor lifts many times its own weight!
Levitation force experiments are in progress

## Slide 19: Defect-related superconducting properties of MgB2 can be tuned by irradiation
Lattice defects are needed for efficient flux pinning

## Slide 20: Summary
Superconducting levitation is attractive for capsule support.
MgB2 is currently the material of choice for levitation.
Non-epitaxial superconducting MgB2 films have been made by
  Mg vapor annealing @850 oC,
  Solid-state diffusion annealing @450-650 oC.
Oxygen impurity is inimical to superconductivity of MgB2.
Quantum levitators can be tuned by defect-induced flux pinning.
Levitation force measurements are in progress.