## Slide 1: Exploring Ionic Liquids as Designer Solvents for Metal Electrodeposition
23rd Target Fabrication Meeting
Annapolis, Maryland
Corie Horwood
Anh Pham, Zach Gavin, Amitesh Maiti,
Vanessa Peters, Michael Stadermann
April 25, 2019

## Slide 2: NIF ignition designs require low-Z ablators and high-Z hohlraums
Beryllium – Low-Z ablator material
DU hohlraums – increase X-rays generated by laser beams
Be
Pt
Physical vapor deposition (PVD) is currently used for making beryllium shells and DU hohlraums
PVD issues: columnar growth, voids, “stickiness”
Electroplating these materials offers a robust pathway for producing small grain, dense materials
3 µm
SEM images: John Bae
10 µm

## Slide 3
Potential
Copper
Silver
Platinum
0 V
Aluminum
Beryllium
Uranium
Plutonium
IL Cation
Electrochemical window of water
Electrochemical window of ionic liquids
Gold
Wide electrochemical window of ionic liquids allow electroplating of several metals of interest for ICF
Electrochemical window of water limited by hydrolysis
No water present ionic liquids
Ionic liquids are difficult to oxidize/reduce, giving large stability window
Reduction potentials for metals
Mn+ + ne- → M
-2.4 V
Standard reduction potentials of metals indicated

## Slide 4: Ionic Liquids (ILs) are salts that are liquid at room temperature
Imidazolium
based
Pyridinium
based
Ammonium based
Requirements
Air/moisture stable
Good conductivity
Electrochemical window to -3 V
Low viscosity
Available to purchase
(no custom synthesis)
Organic cation
Inorganic anion
Possible IL candidates
Cations
Anions
1-Ethyl-3-methylimidazolium trifluoromethanesulfonate
(EMIM OTf)

## Slide 5
Determining the best solvents for electrodeposition requires good understanding of how solvents affect deposition.
anion
anion
metal
Effect of IL cation
Columnar growth
Planar growth
Effect of IL anion
Cation defines electrochemical window
Initial problems
No well-established, reliable reference electrode
Literature on electroplating shows only thin layers
Metals deposited from ILs are often dendritic or contaminated
5µm
5µm
Na
Binding strength of IL anion determines potential that metal ions are reduced
Stability of cation determines negative limit of electrochemical window
Cation affinity for different crystal faces determines preferred growth orientation
Silver deposit contaminated with cation breakdown products
Dendritic silver deposit

## Slide 6: Challenge #1: Developing a reference electrode for controlling potential in electrochemistry experiments
Chart: Potential (V)
oxidizing
reducing
Chart: 
5µm
Na
Silver deposit contaminated with cation breakdown products
Typical reference electrode found to drift by 100+ mV during short experiment

## Slide 7: Precise control of potential is critical and requires developing a reference electrode for use in ionic liquids
Chart: 
Chart: 
A silver wire quasi-reference electrode (QRE), commonly used for IL electrochemistry, shows drift in potential throughout experiment.
A stable reference electrode is required for plating alloys and gradients.
Chart: Potential (V vs Ag2S)
Chart: Potential (V vs Ag2S)
Chart: 
Ferrocene
Cobaltocene
Reference electrode drift
Ferrocene drift

## Slide 8: Ag2S coated Ag wire found to be most stable and reproducible reference electrode for ionic liquids
Ag2S coated Ag Wire
Glass tube
Ionic liquid
PTFE shrink tube
Porous glass frit
Reference electrode (RE) stability is increased by isolating RE in tube with porous frit.
~ 1 mV drift per day over 2-3 month lifetime
  Paper: Horwood, Electrochem. Comm. 88, 105 (2018).
  Patent: Solvent Independent Reference Electrodes for Use with Non-aqueous Electrolytes, 16336–00083–US, 2018.
RE reproducibility is increased by incorporating a well-defined surface coating.
Variation of 57 mV between REs with Ag2S coating (vs. 225 mV variation without Ag2S coating)

## Slide 9: Challenge #2: Measuring diffusion coefficients for metal ions in ionic liquids
300µm
10µm

## Slide 10
Chart: Potential (V vs. Ag2S)
Chart: Potential (V vs. Ag/Ag2S)
Metal ions seem plagued by unusually poor diffusion in IL while redox standards show normal diffusion
EMIM BF4 + 0.2 M Cu OTf
BMP NTf2 + 5 mM Fc + 20 mM CcPF6
Cu2+
+
Diffusion of redox standard is slower
in IL vs. water
Diffusion of Cu2+ is orders of magnitude
slower than redox standard
Diffusion of Ag+ and Cu2+ ions in ionic liquids is ~1000x slower than in water.

## Slide 11
Current decay can be used to measure the diffusion coefficient
Cottrell equation
Chart: 
Slope = 2nFAπ-1/2D1/2C
t1/2
Q
Q = 2nπ -1/2FACoD1/2t1/2
Apply potential
Measure current
Q (charge)
Q(measured)=(constant)(unknown) time
Time
Potential
Current

## Slide 12: Diffusion coefficient varies with ionic liquid anion
Metal ions diffuse 300-6000x slower in ILs vs. water
Copper ions diffusion slower than silver ions
Chart: Diffusion Coefficient (cm2s-1)
| 1 | 3 | 2
Copper diffusion | 4.9241e-08 | 9.1055e-08 | 6.4637e-08
Silver diffusion | 3.4653e-07 | 1.8515e-06
Cu reduction potential | -0.164 | 0.098 | 0.04
Ag reduction potential | 0.053 | 0.301 | 0.245

## Slide 13: Solvated radius may be more influential than viscosity in determining metal ion diffusion in ILs
Chart: 
| 10 | 15 | 8 | 9 | 4.5
Copper | 0.49241 | 0.91055 | 0.64637 | 1.897 | 5.129
Chart: Viscosity vs. diffusion
| 10 | 15 | 8 | 9 | 4.5
 | 4.9241e-08 | 9.1055e-08 | 6.4637e-08 | 7.05e-08 | 3.54e-08
Chart: Copper diffusion coefficients in several ILs
| 10 | 15 | 8 | 9 | 4.5
 | 0.49241 | 0.91055 | 0.64637 | 0.705 | 0.354
+
Cu2+
Cu2+
anion
anion
Cu2+
anion
: viscosity
r: effective solvated radius
How do we measure/estimate r? How many anions are in solvation shell?
Chart: η (Viscosity/mPas)
| 59 | 90 | 85 | 158 | 36 | 33 | 21 | 141
Cobaltocene | 1.2802 | 0.95563 | 0.84564 | 0.62116 | 1.9262 | 4.3926 | 6.1191 | 0.68121

## Slide 14: Solvation of ions in ionic liquids is important for metal ion diffusion and reduction potential
Molecular dynamics simulation of Cu+ in EMIM OTf
Pham et al. J. Phys. Chem. B 2018, 122, 50, 12139-12146.
anion
anion
Copper
Cu+ has a static solvation shell of two anions
Ag+ has a fluid solvation shell of 2-5 anions

## Slide 15: New pulsed potential approach was developed to measure reduction potentials in ionic liquids
Cu reduction
Reduction potential
Cu oxidation
Potential
Log(current)
Intersection → reduction potential
Slope → info on mechanism
Anion has significant effect on reduction potential of metals in ILs
Apply potential
Measure current
Time
Potential
Current

## Slide 16: Strength of metal/anion interaction is a key factor in both reduction potential and diffusion coefficient
Metal ions are harder to reduce in ILs compared to water
Chart: Diffusion Coefficient (cm2s-1)
| 1 | 2
Silver diffusion | 3.4653e-07 | 1.8515e-06
Cu reduction potential | -0.164 | 0.098 | 0.04
Ag reduction potential | 0.053 | 0.301 | 0.245

## Slide 17: Strength of metal/anion interaction is a key factor in both reduction potential and diffusion coefficient
Metal ions are more easily reduced in ILs with better diffusion, indicating weaker binding of anions.
Metal ions are harder to reduce in ILs compared to water
Metal ions diffuse 300-6000x slower in ILs vs. water
Chart: Diffusion Coefficient (cm2s-1)
| 1 | 3 | 2
Copper diffusion | 4.9241e-08 | 9.1055e-08 | 6.4637e-08
Silver diffusion | 3.4653e-07 | 1.8515e-06
Cu reduction potential | -0.164 | 0.098 | 0.04
Ag reduction potential | 0.053 | 0.301 | 0.245
Ideal ILs for deposition have low overpotentials and fast diffusion

## Slide 18: Study of copper and silver deposition has allowed us to better understand electrodeposition in ionic liquids, and move towards choosing appropriate ILs for deposition
5 µm
5 µm
5µm
Change anion for faster diffusion
Change cation for larger crystals
Silver deposited from ionic liquids

## Slide 19: We are using this knowledge to select candidate ILs for electroplating beryllium
Future work:
Beryllium electrodeposition
Need soluble, but weakly bonded, Be precursor
Need IL anion strong enough to solvate Be, but not too strong to inhibit diffusion and reduction
Need cation that promotes planar Be deposits
5 µm
5 µm
5µm
Change anion for faster diffusion
Change cation for larger crystals
Silver