## Slide 1: Ion Beam Analysis of Laser Targets
Target Fabrication Meeting 2019
Swanee J. Shin, L. Bimo Bayu Aji, Sergei O. Kucheyev
April 25, 2019

## Slide 2: Ion beam analysis (IBA) is an important tool to measure elemental composition
RBS : Rutherford Backscattering Spectrometry
ERDA : Elastic Recoil Detection Analysis
NRA : Nuclear Reaction Analysis
PIXE : Particle Induced X-ray Emission
Low Energy
Medium Energy
High Energy
Ion Mass (amu)
Ion Energy (keV)
H
He
Ar
SIMS
LEIS
MEIS
RBS
ERDA
NRA, PIXE, PIGE
Combined with other complementary tools IBA provides critical pre-shot data
W in HDC
Mid Z in opacity samples
Depth profiling of gradient density samples
Low Z contamination
Hydrogen content
Deuterium content
Ion beam analysis is widely used for targets metrology

## Slide 3: Ion beam analysis is based on physical interaction between incident ions and target atoms
Ernest Rutherford (1871-1937)
Known as “the father of nuclear physics”
Discovered alpha, beta radioactivity
Discovered atomic nucleus
Discovered proton
Au foil experiment
Rutherford model
Form the basis of
- Ion beam analysis - Atomic model
- Nuclear reactions
- Manhattan project
- LLNL

## Slide 4: Ion beam facility at LLNL allows probing materials with up to 4 MeV/charge ions
Control console
Charging system
Acceleration tube and gas bottles
Pressure vessel &
beam lines
Gas bottles
Pressure vessel
Acceleration Tube
Bending magnet
Analysis beam line
Charging chain

## Slide 5: The ion beam facility is equipped with various diagnostics for state-of-the-art ion beam analysis
Analysis chamber
Microscope
X-ray detector
164◦ detector
Electron
gun
RGA
Annular
detector
RGA: Residual Gas Analyzer for detecting gaseous species
X-ray detector: Used for PIXE
Annular, 164◦, and glancing angle detectors: Used for RBS, NRA
PIGE port
ERDA
detector
Sputter gun
port
Microbeam
lens

## Slide 6: RBS is used to measure W concentration in HDC capsule
[W] = 0.27 at.%
Atomic mass: 184W
Composition
(scattering cross section)
Depth
(stopping power)
Atomic mass: 12C
Very large scattering cross section of W allows:
- Easy detection of low W concentration
- Capable of resolving ~0.02 at.% difference
Target atomic mass
(kinematic factors)
2 MeV He+
ions
Detector
Sample holder for
broad-beam capsule
measurements
capsule

## Slide 7: RBS is used to measure Fe and Mg atomic areal densities in FeMg opacity targets
Opacity target geometry
Beam energy and current were optimized
Advanced simulation method with accurate stopping powers was used
Mg
Fe
- Areal densities of Fe and Mg were independently measured
Deviation of 3% or less for 3 independent measurements
Results are consistent with 2 independent RBS measurements off-site
Depth
3 MeV He+
ions
Detector
~ 300 nm
Related presentation: H. Huang, Thu 11:00 AM

## Slide 8: Proton beam RBS can measure composition profiles over large depths
Multiple scattering from are all taken into account
(Total film thickness, SEM image : ~8.5 um)
W
Be
~5 um
W spectrum
~7.6 um
BeW alloy
Thickness calculation assumes that the density changes linearly as a function of the W:Be ratio of the alloy
Depth Profile

## Slide 9
Light (low Z) element in heavy (high Z) matrix is typically considered non-ideal case for RBS
Resonance scattering (enhanced cross section) could be used to probe low Z elements
12C(p,p)12C ion scattering cross section
Incident energy (KeV)
Cross section (mb/sr)
1.75 MeV
Non-Rutherford (resonant) backscattering could be used
to detect C contamination on a machined Fe surface
RBS spectrum of carbon substrate
using 1.75 MeV proton ion beam
1.75 MeV
- Without resonant peak, even 10 at.% C in Fe matrix is difficult to detect
- With resonance peak, 2-3 at.% C on Fe matrix is readily detected
Related presentation: C. Castro, Wed 9:50 AM

## Slide 10
- Hydrogen concentration was measured as a function of ion dose
- Combined with RBS, we were able to measure C, O, H concentration in GDP
ERDA (Elastic Recoil Detection Analysis) could measure depth profiles of hydrogen in targets
Evolution of hydrogen concentration in Xe implanted GDP for RadChem experiments

## Slide 11
RBS, ERDA, and RGA are used to measure decomposition kinetics of alpha-irradiated Stycast
Complete compositional analysis from RBS+ERDA:
C 1.00 H 0.96 N 0.06 O 0.10
RBS
Related presentation: M. Wilson, Wed 1:50 PM
RGA
ERDA

## Slide 12: PIXE (Particle Induced X-ray Emission) provides excellent low- & mid-Z detection sensitivity
PIXE
C K
O K
Energy (keV)
Energy (keV)
Yield
Yield
The principle is similar to EDS, but PIXE has better sensitivity
C K
O K
EDS
GDP
GDP

## Slide 13
NRA could be used for isotope profiling (D in HDC capsule)
3He NRA for deuterium profiling
2D + 3He = 1H + 4He, Q = 18.4 MeV
Increase in ion energy (inverse kinematics), most energy taken by 1H
Integrate 1H peak to calculate D concentration
0.8 MeV 3He NRA of CD
Incident energy (MeV)
Cross section (mb)
D(3He,p)4He
scattering cross section
C(3He,3He)C
(RBS)
diagnostics
pulse
D(3He,4He)H
D(3He,1H)4He
0.8 MeV

## Slide 14: Ion Beam Analysis is flexible and can provide crucial elemental information regarding target components
RBS Strength - Quantitative without standards - Depth-profiling - Non-destructive - Simple, fast, and direct | Weakness - No phase or microstructure information - Moderate sensitivity for light impurities - Expensive and rare facility
ERDA Depth profile of H, D | 
nRBS Selectively enhanced detection sensitivity (isotope specific) | 
PIXE Similar to EDS but with better sensitivity. Good for low- & mid-Z atom detection in heavy matrix | 
NRA Detect products of nuclear reactions (isotope specific) |