## Slide 1: Recent Foams and Aerogels Development at Los Alamos National Laboratory
LA-UR-19-23279
23rd Target Fabrication Specialists’ Meeting
April 23-26 2019, Annapolis MD
Chris Hamilton, Christina Hanson, Stephanie Edwards, and John Oertel

## Slide 2: Outline
DVB aerogel, tantalum oxide
  lower d, Doped DVB, Ta2O5
Polyimide aerogels, for targets
  possible candidate for DS, MShock
PI aerogel: AM R&D, non target fab
  additive manufacturing
  stockpile materials replacement
  air-buoyant solids
  energetic materials
Silica aerogels for Cherenkov detectors
  attaining high densities, low densities
  critical parameters: clarity, light collection

## Slide 3: DVB Aerogel
polyHIPE still problematic
  voids, shrinkage at low densities
Reduced density DVB aerogel
  for Double Shell, MARBLE?
  reduced d from 30 mg/cm3 to 16 mg/cm3
Doped full-d plastics
  halogens, silicon
Doped DVB aerogel
  ~100 mg/cm3 Si doped, Cl doped (LDRD)
  3% Cl, 3% I doped less robust (MShock)
Checked out Stephanie Edwards’ poster?
Double Shell parts
DVB in MARBLE VC target

## Slide 4: Tantalum Oxide Aerogel, Ti doped SiO2
1:5 TiO2:SiO2
  Chunky/ smooth
Ta2O5 aerogel: high z, low d
  for DS, other applications
  200 mg/cm3, 400 mg/cm3
Checked out Stephanie Edwards’ poster?
Machined tantalum oxide aerogel sphere
tantalum oxide aerogel. ~250 mg/cm3

## Slide 5
Polyimide Aerogel
2 mm
  Dianhydride + diamine
  Polyamic acid oligomers imidized
    thermally or chemically
  Crosslinking to form gels
    triamines, acid chlorides, etc
  Wide variety of monomers:
    tailored properties
2 mm
M.A.B. Meador et al., ACS Appl. Mater. Interfaces 2015, 7, 1240.

## Slide 6
2 mm
Broad density range
  17-120 mg/cm3 (GA has done lower, we have done higher)
Machinable
  DVB replacement for Double Shells?
  replacement for doped DVB for Mshock
Tunable stoichiometry?
2 mm
Polyimide Aerogel for Targets
Machined PI aerogel, 100 mg/cm3 for MShock target

## Slide 7
Polyimide Aerogel AM: can we print it?
2 mm
Introduce acrylate functionality
  Allows photopolymerization
  At the cost of lost thermal stability
  Thermal imidization
from M. Hegde et al., Adv. Mater. 2017, 29, 1701240.

## Slide 8
Polyimide Aerogel AM: can we print it?
2 mm
Introduce acrylate salts
  Allows photopolymerization
  At the cost of lost thermal stability
  Unless…
M. Herzberger et al., ACS Macro Lett. 2018, 7, 493.
D. A. Rau et al., ACS Appl. Mater. Interfaces 2018, 10, 34828.

## Slide 9
Checked out Christina Hanson’s poster?!
Acrylate functionalized monomers
  photopolymerized
  supercritical drying
  thermal imidization, shrinkage
Direct ink write?
Thermally treated PI aerogel
3D printed polyamic acid gel
Polyimide Aerogel AM: can we print it?

## Slide 10: Polyimide Aerogels for Other Applications
Stockpile materials replacement
  APO-BMI, alternate drying methods
LDRD- buoyant solids
  SiO2 not viable
  alternate drying strategies, composites
Energetics: switchable safing
  eventually: sensitized, MIC, other composites
GS
10 cm
aerogel detonation? L: before, R: after
PI aerogel hemi, 120 mg/cm3
http://asd.gsfc.nasa.gov/

## Slide 11: SiO2 Aerogel Cherenkov detectors
Cherenkov radiation
  gas, liquid, aerogels in between
  refr. index (density) determines energy threshold
ACD fielded on Cygnus at NNSS, now Z
Cherenkov radiator 1
OAP
OAP
PMT
4” Tungsten
Collimator
X-rays
Cherenkov radiator 2
Y. Kim et al., Rev. Sci. Instrum. 2016, 87, 11E723.

## Slide 12: SiO2 Aerogel Cherenkov detectors
Density range 10 to 425 mg/cm3
  thermal sintering required for high d
  chemistry: TMOS, MeSi51, CS
  critical parameter: optical clarity
  Machining, solvents
Aerogel Cherenkov radiators, L to R: density 70, 164, 285, 348, 426 mg/cm3
M. Tabata et al., Nucl. Instrum. Meth. A 2012, 668, 64.
I.L. Rasmussen, J. Physique Colloq. 1989, C4, C4-221 (2nd Int. Symp. Aerogels 1988).

## Slide 13: SiO2 Aerogel Cherenkov detectors
348 mg/cm3 aerogels, L: machined; R: as cast.
More info
  thermal sintering
  Machining, solvent?
From I.L. Rasmussen, J. Physique Colloq. 1989, C4, C4-221 (2nd Int. Symp. Aerogels 1988).

## Slide 14: Summary
Plethora of foams:
  DVB, Ta2O5, PI, SiO2
Acknowledgments
  LANL MST-7 Target Fab team
  Miles Beaux, Bryce Tappan
  Matt Lee, Kyle Cluff
  Hans Herrmann, Yongho Kim
  target fab colleagues at LLNL, GA
References:
  M.A.B. Meador et al., ACS Appl. Mater. Interfaces 2015, 7, 1240.
  M. Hegde et al., Adv. Mater. 2017, 29, 1701240.
  M. Herzberger et al., ACS Macro Lett. 2018, 7, 493.
  D. A. Rau et al., ACS Appl. Mater. Interfaces 2018, 10, 34828.
  Y. Kim et al., Rev. Sci. Instrum. 2016, 87, 11E723.
  I.L. Rasmussen, J. Physique Colloq. 1989, C4, C4-221.

## Slide 16
Future Directions and Materials
Double Shells, Revolver, other future platform requirements
  Precisely controlled density- density gradients
  Pure metals, mixed metals, compositional gradients
  Spherical geometries- radial density gradients
  Structural foams require strength
Bijels: past and present
  Tunability, flexibility
  Bijel templated, polymer cast metal foams
  True metal particle stabilized bijels
  Bijel templated ultralow density carbon
Recent AM advances for metals
  Printed metal foams: density gradients